LABFLOW / SCIENTIFIC PROJECT REPORT Mixed-Cation Validation Report Editable local report test PRJ-2026-014-R01 ¦ 2026-08-03 Matteo Ginesi ¦ CHOSE — Centre for Hybrid and Organic Solar Energy Pending researcher signature

Keywords: perovskite, mixed-cation, validation

| 01 | Executive Snapshot ¦ decision-ready project summary |
| --- | --- |

Executive summary

The leading formulation remains FA0.90MA0.10.

Research objectives

Compare MA/FA ratios and identify the most stable high-efficiency device stack.

| BEST PCE | MEAN PCE | BEST STABILITY | MEAN VOC | OPEN ISSUES |
| --- | --- | --- | --- | --- |
| 21.28% / S08 | 19.79% | 95% | 1.09 V | 3 |

| 02 | Materials, Process and Experiments ¦ traceable preparation |
| --- | --- |

Methodology

Versioned preparation, mapped JV data and deterministic comparison.

## Solution Review / SOL-B04

| Component | Function | Quantity | Composition |
| --- | --- | --- | --- |
| DMF | Primary solvent | 1.60 mL | 80% v/v |
| DMSO | Co-solvent | 0.40 mL | 20% v/v |
| FAI | A-site solute | 365.3 mg | 90 mol% |
| MAI | A-site solute | 39.7 mg | 10 mol% |
| PbI2 | Lead halide | 1152.5 mg | 1.00 eq |

## Device Stack / STK-003 v2

| Order | Material | Function | Thickness |
| --- | --- | --- | --- |
| 05 | Au | Back contact | 80 nm |
| 04 | Spiro-OMeTAD | Hole transport | 180 nm |
| 03 | FA/MA perovskite | Photoactive absorber | 540 nm |
| 02 | SnO2 | Electron transport | 32 nm |
| 01 | Glass / FTO | Substrate + front contact | 2.2 mm |

## Experiment Coverage

| Experiment | Samples | Process | Measurements | Status |
| --- | --- | --- | --- | --- |
| EXP-041 | S01-S03 | 100 C / 30 min | 6 | Reviewed |
| EXP-052 | S04-S05 | 105 C / 25 min | 4 | Reviewed |
| EXP-067 | S06-S08 | 100 / unit missing | 24 | Review |

## Data-quality review

| Severity | Issue | Effect |
| --- | --- | --- |
| Error | Device count mismatch | Resolve before final interpretation |
| Warning | Annealing unit missing | Comparison retained with caveat |
| Warning | Solution provenance incomplete | Causal inference blocked |

| 03 | Complete Results ¦ source-aligned measurements |
| --- | --- |

## PCE performance overview

| Sample | Formulation | PCE (%) | Stability (%) | Hysteresis (%) |
| --- | --- | --- | --- | --- |
| S01 | FA0.85MA0.15 | 19.15 | 89 | 3.2 |
| S02 | FA0.85MA0.15 | 20.16 | 91 | 2.8 |
| S03 | FA0.80MA0.20 | 18.94 | 85 | 4.1 |
| S04 | FA0.90MA0.10 | 21.1 | 94 | 2.1 |
| S05 | FA0.90MA0.10 | 19.9 | 92 | 2.5 |
| S06 | FA0.75MA0.25 | 17.36 | 78 | 5.9 |
| S07 | FA0.85MA0.15 | 20.44 | 90 | 2.7 |
| S08 | FA0.90MA0.10 | 21.28 | 95 | 1.9 |

## Complete measurement table

| Sample | Formulation | Batch | Voc (V) | Jsc | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- | --- |
| S01 | FA0.85MA0.15 | B01 | 1.08 | 22.7 | 78.1 | 19.15 |
| S02 | FA0.85MA0.15 | B01 | 1.1 | 23.2 | 79 | 20.16 |
| S03 | FA0.80MA0.20 | B02 | 1.07 | 22.9 | 77.3 | 18.94 |
| S04 | FA0.90MA0.10 | B03 | 1.12 | 23.5 | 80.2 | 21.1 |
| S05 | FA0.90MA0.10 | B03 | 1.09 | 23 | 79.4 | 19.9 |
| S06 | FA0.75MA0.25 | B04 | 1.05 | 21.8 | 75.8 | 17.36 |
| S07 | FA0.85MA0.15 | B05 | 1.11 | 23.1 | 79.7 | 20.44 |
| S08 | FA0.90MA0.10 | B06 | 1.13 | 23.4 | 80.5 | 21.28 |

| Sample | Stability (%) | Hysteresis (%) |
| --- | --- | --- |
| S01 | 89 | 3.2 |
| S02 | 91 | 2.8 |
| S03 | 85 | 4.1 |
| S04 | 94 | 2.1 |
| S05 | 92 | 2.5 |
| S06 | 78 | 5.9 |
| S07 | 90 | 2.7 |
| S08 | 95 | 1.9 |

Researcher interpretation

S08 remains the current performance leader.

| 04 | Evidence-Linked Findings ¦ advisory review |
| --- | --- |

AI-assisted findings are simulated and remain separate from researcher conclusions.

| Score | Finding | Detail | Evidence | Status |
| --- | --- | --- | --- | --- |
| 96 | FA0.90MA0.10 is the strongest candidate | S04 and S08 lead both PCE and stability, with the lowest hysteresis. | S04, S08 · 7 metrics | accepted |
| 91 | S06 is a multi-metric outlier | PCE, fill factor and stability are jointly below the robust cohort range; review fabrication notes before exclusion. | S06 · IQR + robust z | review |
| 88 | Batch effect is smaller than formulation effect | Within-batch variation is limited compared with the shift between formulations. | Grouped comparison | accepted |
| 84 | Stability and hysteresis are inversely associated | Lower hysteresis appears in the most stable devices; the sample count does not support a causal claim. | Spearman preview | review |
| 78 | Two metadata gaps limit reproducibility | Humidity during coating and elapsed time before annealing are missing for B04 and B05. | Process records | action |

| 05 | Researcher Decision ¦ interpretation and boundaries |
| --- | --- |

Discussion

The current cohort supports validation but not causal inference.

Conclusions

S04 and S08 proceed to validation; S06 remains under review.

Limitations

Small demonstration cohort; no causal inference.

| 06 | Additional notes |
| --- | --- |

Additional notes

The author requested one additional validation run.

| 07 | Provenance and Approval ¦ evidence classes and final state |
| --- | --- |

| Evidence class | Origin | Control |
| --- | --- | --- |
| Raw | Local measurement files | Preserved |
| Calculated | Deterministic transformations | Reproducible |
| Researcher | Objectives, interpretation and approval | Human authored |
| AI | Local demonstration rules | Researcher review |

## Source appendix

batch_B03_forward.csv - source-aligned JV measurements; process_metadata.yaml - process metadata; SOL-B04 - reviewed solution snapshot; STK-003/v2 - versioned device architecture.

Approval / signature state

Pending researcher signature